PP (POLYPROPYLENE) STRAP

Material   			PP – (Polypropylene)

Width  				9mm to 19mm in width options available

Thickness 			0.6mm to 1.0mm

Printing			Sterio Printing Avaliable

Breaking Strength Range - 	50kg to 200kg

FOR FULLY AUTOMATIC ALL GRADE

Core Diameter  	203mm (OD), 187mm (Width)

Core Weight 		700gm

Standard packing	8 kg Net Weight, Can Be Change as per requirement

FOR HEAT SELABLE SEMI AUTOMATIC ALL GRADE

Core Diameter  	203mm (OD), 165mm (Width)

076mm (OD), 165mm (Width)

Core Weight 		150gms, 600gms, 700gms

Standard packing	3 kg Net Weight, Can Be Change as per requirement

KARAM PP straps are available from 9mm to 19mm They are eco-friendly, food safe and ecologically compatible. On request, we will be happy to produce it for you in other colors and Printing option on it as well. PP strapping material is particularly suitable for strapping packages, cartons or other containers, as well as lighter pallets.

APPLICATION

General logistics (boxes of corrugated cardboard, styrofoam, plastic)

Printing industry (newspaper, magazines)

Corrugated cardboard industry (folding boxes, cut-outs)

Tins and bottles of plastic, aluminum and cardboard

Construction and container (furniture, wooden slats, tiles and bricks)

Food industry (meat, fish, poultry in folding boxes or styrofoam)